## Slide 1
Potential for Enhancement of
Enzymatic Hydrolysis of Sugar Maple (Acer saccharum)
Muhammet Uygut, Derek Corbett, Christopher Wood, Matt Zelie, Biljana Bujanovic
Introduction and Motivation
The efficient and complete removal of carbohydrates from lignocellulosics (LCs) as simple monomeric sugars is one of the “holy grails” of contemporary research in the area of biomass utilization. Enzymatic hydrolysis (EH) is one well researched method to produce monomeric sugars from LC cellulose and hemicelluloses. However, EH is plagued by poor yields due to the inaccessibility and high degree of crystallinity of native cellulose. In this work, electron beam irradiation (EBI), acetone:water (9:1) extraction (AWE), hot water extraction (HWE) with/without subsequent acetone:water wash (AW), and combinations of each are investigated and compared as pretreatments to improve the enzymatic hydrolysis of sugar maple (Acer saccharum, SM).
EBI has been proposed as a method to reduce the crystallinity of cellulose to improve EH1,2. HWE of hardwoods has been used to remove easily accessible hemicelluloses as well as a portion of lignin3. HWE has further been shown to increase delignification efficiency in subsequent pulping processes. AWE has been reported as efficient in lignin dissolution from HW-extracted hardwoods4. Decreased crystallinity of cellulose, removal of lignin and improved reactivity was expected to improve EH.
Experimental
EBI was performed at IBA Industrial in Edgewood, NY for irradiation using a 250kW, 3.0 MeV Dynamitron EB accelerator. Total energy dosages were 250, 750 and 1000kGy (SUNY-ESF; Dr. Mark Driscoll’s group).
HWE was performed in an M/K digester at 160°C for 2 hrs (4:1 liquor to wood) with two water washes: 80°C, 20 min.
AW washes were performed at 120°C for 45 min (4:1 L/W; 9:1 acetone:water) with one water wash: 80°C, 20 min.
AWE of SM and EBISM was performed by ultrasonication (20:1 L/W; 9:1 acetone:water; 2 hours) (Branson 3510).
Lignin was determined by modified Klason procedure5.
EH was performed at 50°C with constant agitation, using 5g of sample, 100mL of 50mM citrate buffer solution (pH 5), 0.2 mL CTec2, and 0.1 mL HTec2 enzymes (Novozymes). Sampling every 6 hours. (HWE and HWE AW tests on SM were done in 12 L reactor; same conditions; 1 hr samples).
Sugar content determined with Waters HPLC system (1525 pump, 2707 autosampler, 2414 RI detector). Total sugars refers to sum of glucose, xylose, arabinose and cellobiose.
Results of Total Mass Removal Experiments
Conclusions and Future Work
The most efficient pretreatment for EH tested in this work was EBI at 250 kGy followed by HWE.
Acetone water extraction does not positively impact EH efficiency for EBI SM.
HWE can achieve EH improvements approximately equivalent to that of 750 kGy EBI.
For EBI SM (no pre-extraction), treatment at EH conditions with no enzymes can yield almost 50% of the yield observed with enzyme based on total mass solubilized. However, the composition of this fraction is unknown.
If HWE is used, EBI above 250 kGy is not recommended as incremental improvement in EH efficiency does not justify the cost of higher energy used.
Further analysis of EH based on sugars in treated wood determined by HPLC will be undertaken in future studies.
HWE followed by EBI will be investigated.
Figure 1: While the highest carbohydrate yield was achieved after 1000 kGy with HWE, the minimal improvement over 250 kGy with HWE leads us to recommend EBI 250 kGy followed by HWE as the most efficient pretreatment for EH.
Chart: Irradiation Level (kGy)
| 0 | 250 | 750 | 1000
Native | 0.062577 | 0.10637 | 0.28354 | 0.38925
AWE | 0.085291 | 0.2514 | 0.35634
HWE | 0.26913 | 0.38925 | 0.38787 | 0.4205
HWE_AW | 0.28898 | 0.21695 | 0.2187 | 0.22632
Chart: Native SM
| 0 | 0 | 6 | 6 | 12 | 12 | 18 | 18 | 24 | 24 | 30 | 30 | 42 | 54 | 54 | 72 | 72 | 72 | 72
0 kGy Native | 0.027023 | 0.043211 | 0.053228 | 0.062851 | 0.058986 | 0.066276 | 0.062376 | 0.065515 | 0.06375 | 0.0638 | 0.061331 | 0.065071 | 0.063982 | 0.059449 | 0.064098 | 0.062282 | 0.063947 | 0.060784 | 0.063296
250 kGy Native | 0.028752 | 0.069983 | 0.076572 | 0.079288 | 0.079942 | 0.086782 | 0.087665 | 0.086289 | 0.0948 | 0.097887 | 0.094834 | 0.10247 | 0.099473 | 0.10299 | 0.1096 | 0.11081 | 0.10206
750 kGy Native | 0.046459 | 0.02428 | 0.1339 | 0.13167 | 0.16516 | 0.15526 | 0.19641 | 0.21054 | 0.21197 | 0.22047 | 0.24862 | 0.2178 | 0.23143 | 0.25482 | 0.27731 | 0.2755 | 0.291 | 0.29034
1000 kGy Native | 0.058352 | 0.06907 | 0.18122 | 0.15217 | 0.24894 | 0.25588 | 0.28539 | 0.24199 | 0.27441 | 0.31532 | 0.28941 | 0.32997 | 0.32819 | 0.39246 | 0.35073 | 0.33309 | 0.42506 | 0.44814
Chart: Hot-water extracted SM
250 kGy | 0.071415 | 0.071809 | 0.18277 | 0.1944 | 0.2398 | 0.25544 | 0.26687 | 0.26152 | 0.27667 | 0.26929 | 0.28215 | 0.30043 | 0.31367 | 0.30162 | 0.30984 | 0.32037 | 0.33328 | 0.3356 | 0.33374 | 0.33654
750 kGy | 0.094888 | 0.066086 | 0.19884 | 0.17758 | 0.25446 | 0.27206 | 0.30294 | 0.2376 | 0.29036 | 0.24711 | 0.35429 | 0.34453 | 0.3687 | 0.34074 | 0.3928 | 0.38808 | 0.37763 | 0.41452 | 0.34016 | 0.41916
1000 kGy | 0.11505 | 0.060079 | 0.22262 | 0.19825 | 0.26264 | 0.29889 | 0.31762 | 0.28279 | 0.32754 | 0.29262 | 0.37088 | 0.37611 | 0.3807 | 0.33136 | 0.40497 | 0.35549 | 0.43649 | 0.42499 | 0.43638 | 0.38413
Chart: Time (hr)
| 0 | 0 | 6 | 6 | 12 | 12 | 18 | 18 | 24 | 24 | 30 | 30 | 42 | 54 | 54 | 72 | 72 | 72 | 72
0 kGy Native | 0.027023 | 0.043211 | 0.053228 | 0.062851 | 0.058986 | 0.066276 | 0.062376 | 0.065515 | 0.06375 | 0.0638 | 0.061331 | 0.065071 | 0.063982 | 0.059449 | 0.064098 | 0.062282 | 0.063947 | 0.060784 | 0.063296
250 kGy Native | 0.028752 | 0.069983 | 0.076572 | 0.079288 | 0.079942 | 0.086782 | 0.087665 | 0.086289 | 0.0948 | 0.097887 | 0.094834 | 0.10247 | 0.099473 | 0.10299 | 0.1096 | 0.11081 | 0.10206
750 kGy Native | 0.046459 | 0.02428 | 0.1339 | 0.13167 | 0.16516 | 0.15526 | 0.19641 | 0.21054 | 0.21197 | 0.22047 | 0.24862 | 0.2178 | 0.23143 | 0.25482 | 0.27731 | 0.2755 | 0.291 | 0.29034
1000 kGy Native | 0.058352 | 0.06907 | 0.18122 | 0.15217 | 0.24894 | 0.25588 | 0.28539 | 0.24199 | 0.27441 | 0.31532 | 0.28941 | 0.32997 | 0.32819 | 0.39246 | 0.35073 | 0.33309 | 0.42506 | 0.44814
Chart: Time (hr)
| 0 | 0 | 6 | 6 | 12 | 12 | 18 | 18 | 24 | 24 | 30 | 30 | 42 | 54 | 54 | 72 | 72 | 72 | 72
0 kGy Native | 0.027023 | 0.043211 | 0.053228 | 0.062851 | 0.058986 | 0.066276 | 0.062376 | 0.065515 | 0.06375 | 0.0638 | 0.061331 | 0.065071 | 0.063982 | 0.059449 | 0.064098 | 0.062282 | 0.063947 | 0.060784 | 0.063296
250 kGy Native | 0.028752 | 0.069983 | 0.076572 | 0.079288 | 0.079942 | 0.086782 | 0.087665 | 0.086289 | 0.0948 | 0.097887 | 0.094834 | 0.10247 | 0.099473 | 0.10299 | 0.1096 | 0.11081 | 0.10206
250 kGy AWE | 0.020319 | 0.014155 | 0.060429 | 0.054873 | 0.049452 | 0.071788 | 0.053398 | 0.065873 | 0.077221 | 0.073492 | 0.097611 | 0.061903 | 0.061444 | 0.083827 | 0.084847 | 0.088216 | 0.089562 | 0.078539
250 kGy HWE | 0.071415 | 0.071809 | 0.18277 | 0.1944 | 0.2398 | 0.25544 | 0.26687 | 0.26152 | 0.27667 | 0.26929 | 0.28215 | 0.30043 | 0.31367 | 0.30162 | 0.30984 | 0.32037 | 0.33328 | 0.3356 | 0.33374 | 0.33654
250 kGy HWE-AW | 0.042861 | 0.041322 | 0.12097 | 0.1257 | 0.16391 | 0.17135 | 0.18818 | 0.18191 | 0.17731 | 0.18094 | 0.14229 | 0.17875 | 0.2145 | 0.19672 | 0.21322 | 0.20672 | 0.21547 | 0.22193 | 0.21864 | 0.21177
Effect of Pretreatment on EH of
SM EBI 250 kGy
Figures 5 and 6: Electron beam irradiation improves enzymatic hydrolysis, however, HWE (0 kGy) achieves approximately the same result as 750 kGy EBI. HW-extracted SM achieves the best result among the pre-extraction types while any extraction with acetone reduces the EH efficiency. In both figures native SM is included as control (0 kGy Native).
Effect of EBI on EH of SM in comparison
to effect of HWE
Chart: g/g substrate
| SM | 250 | 750 | 1000 | 250 HWE | 750 HWE | 1000 HWE
No Enzyme | 0.0306 | 0.0534 | 0.1465 | 0.1786 | 0.1032 | 0.1158 | 0.1205
With Enzyme | 0.0679 | 0.1165 | 0.3215 | 0.4363 | 0.3278 | 0.3498 | 0.39953
Total Carbs After 72Hr | 0.062577 | 0.10637 | 0.28354 | 0.38925 | 0.38925 | 0.38787 | 0.4205
Figure 7: For native SM and EBI SM, on average 44.4% of the material solubilized with enzyme present (red) can be solubilized without any enzyme at all (blue). That number is only 31.5% for HW-extracted samples. This is due to HW-extracted SM having less easily extractible material remaining after HWE. Total mass removed agreed well with final sugar concentrations.
Figures 2 and 3: For native sugar maple, EB irradiation greatly improves EH efficiency. However, the effect of EB irradiation is not nearly as profound on samples when HWE is performed after EBI treatment.
Total Carbohydrates in Hydrolysate After 72 Hours for All Samples Tested
Comparison of Effects of EBI and EBI Followed by HWE on EH of SM
Chart: g sugar/g extracted material
| 0 | 0 | 6 | 6 | 12 | 14 | 18 | 18 | 24 | 24 | 30 | 30 | 42 | 42 | 54 | 54 | 72 | 72 | 72 | 72
Glucose | 0.022803 | 0.02185 | 0.11055 | 0.12007 | 0.15874 | 0.17433 | 0.18564 | 0.18071 | 0.19188 | 0.18667 | 0.19846 | 0.2102 | 0.22474 | 0.21222 | 0.22006 | 0.22995 | 0.23952 | 0.23913 | 0.23604 | 0.24294
Xylose | 0.031038 | 0.031046 | 0.072228 | 0.074325 | 0.081058 | 0.081111 | 0.081226 | 0.080814 | 0.084788 | 0.082619 | 0.083689 | 0.090238 | 0.088933 | 0.089406 | 0.08978 | 0.090424 | 0.093755 | 0.096468 | 0.097693 | 0.093605
Cellobiose | 0.017574 | 0.018913 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Individual Sugars in Hydrolysate
(SM EBI 250 kGy HWE)
Time (hr)
Time (hr)
Figure 4: The production of individual sugars over time during EH of SM EBI 250 kGy EBI.
Time (hr)
Table 1: HWE and AW yields for SM of different EBI dosages.
Special thanks to Dr. Mark Driscoll’s group for providing the EBI SM samples and to Mr. Bob Kelly for help with sample preparation. Thanks to McEntire Stennis: “Enhancing production of uniform high purity lignin” and “Thermoplastic blends based on biorefinery lignin.”
References:
1. Cheng, K.; Barber, V. A.; Driscoll, M. S.; Winter, W. T.; Stipanovic, A. J. “Reducing Woody Biomass Recalcitrance by Electron Beams, Biodelignification and Hot-Water Extraction.” Journal of Bioprocess Engineering and Biorefinery 2013, 2 (2), 143–152 DOI: 10.1166/jbeb.2013.1048.
2. Driscoll, M. S.; Stipanovic, A. J.; Cheng, K.; Barber, V. A.; Manning, M.; Smith, J. L.; Sundar, S. “Ionizing radiation and a wood-based biorefinery.” Radiation Physics and Chemistry 2014, 94, 217–220 DOI: 10.1016/j.radphyschem.2013.05.045.
3. Amidon, T. E.; Wood, C. D.; Shupe, A. M.; Wang, Y.; Graves, M.; Liu, S. “Biorefinery: conversion of woody biomass to chemicals, energy and materials.” Journal of Biobased Materials and Bioenergy 2008, 2 (2), 100–120.
4. Gong, C.; Goundalkar, M. J.; Bujanovic, B. M.; Amidon, T. E. “Evaluation of Different Sulfur-Free Delignification Methods for Hot-Water Extracted Hardwood.” J. Wood Chem. Technol. 2012, 32 (2), 93–104 DOI: 10.1080/02773813.2011.607534.
5. Dence, C. W. The Determination of Lignin. In Methods in Lignin Chemistry; Lin, D. S. Y., Dence, P. E. D. C. W., Eds.; Springer Series in Wood Science; Springer Berlin Heidelberg, 1992; pp 33–61.
EBI (Kgy) | HWE Yield | AW Yield
0 | 77.0 | 92.7
250 | 76.2 | 92.8
750 | 67.2 | 91.1
1000 | 64.3 | 88.4
HWE and AW Reactor Yields (% OD)
Recommended Treatment